## Slide 1: In silico polymer science Мезоскопическое моделирование полимерных систем: от биологии до материаловедения
Алексей Гаврилов (aka gavrilov@lomonosov)
Владимир Рудяк (aka vurdizm@lomonosov)
Александр Чертович (aka chertov@lomonosov)
Физический факультет МГУ
Лаборатория микроструктурированных полимерных систем

## Slide 2
Экспоненциальный рост вычислительных мощностей + большие данные + машинное обучение
In silico (лат.) означает проведение виртуальных экспериментов с заранее неизвестным результатом
Введение

## Slide 3
Введение
Уже сегодня in silico эксперименты стали полноправным третьим способом научного исследования, заняв место между традиционными лабораторными экспериментами и аналитическими теориями
Очень скоро такие исследования будут доминировать во всех областях науки и техники

## Slide 4
План доклада
Модель организации хроматина
Реалистичные микрогели
Самоорганизация по ходу проведения полимеризации
Микрофазное расслоение

## Slide 5
DPD:
up to ~10 μm
up to ~1 ms
Пространственно-временные масштабы в компьютерном моделировании
Notes: time and space scales in molecular modeling. All simulation methods and techniques could be divided into several groups according to available time and space scales. And as you can see there are so many methods that one must always keep in mind what kind of effects onw wants to study. This is actually rather crucial because theoretically any effect can be captured by QM simulations… but it’s just technically impossible to have a system of a relevant size and study the system behavior for a reasonable time. Since polymers are large molecules a lot of interesting action in polymer systems happens on rather large time and length scales we are interested in the methods that can capture them. Such methods can be called coarse-grained methods and DPD is one of them.

## Slide 6: Диссипативная динамика частиц (DPD)
Расстояние
Потенциал
Леннард-Джонс
ДДЧ
Модель «бусинки на пружинках»

## Slide 7
Строение хроматина: открытые вопросы
Как все устроено на уровне между нуклеосомами и хромосомными территориями?

## Slide 8: Хроматин: введение “насыщающихся” взаимодействий
В живой природе существует огромное множество специфических взаимодействий, основанных на распознавании последовательности или поверхности, они работают по принципу «ключ-замок»
На огрубленном уровне все такие взаимодействия можно представить как «насыщающиеся», как бы с фиксированной «валентностью».
Мономерное звено
Notes: Let’s move to dissipative particle dymanics. It’s a coarse-grained version of molecular dynamics. This tech- nique is based on the simulation of soft spheres, whose mo- tion is governed by certain collision rules. all particles interact by three forces. It was shown that the dissipative force and the random force have to satisfy a certain relation in order that the system has the statistical mechanics corresponding to the canonical en- semble with a temperature related to the relative amplitudes of the random and dissipative interactions.
As compared to usual molecular dynamics simulations, for example with Lennard-Jones atoms, the major advantage of the DPD method is its soft interaction potential FC. Such a soft force can be considered as a mean effective force arising from averaging the interactions between the groups which compise each beads over time and orientations. Soft potential allows for a much larger timestep than is commonly used in usual MD simulations because the force does not diverge at any distance.

## Slide 9
Объемные взаимодействия: Насыщающиеся взаимодействия:
Переход газ-жидкость Переход одноатомный-двухатомный газ
reaction
Однако, полимер это соединенные в единую цепь молекулы, и поэтому они обеднены трансляционной энтропией. В таких системах для гомополимера возможен переход клубок-глобула.
Объемные и насыщающиеся взаимодействия: какая разница?

## Slide 10
Блок A – слипающиеся звенья
Block B –
неслипающиеся
В большинстве эукариот (напр. Drosophila) уровень ацетилирования напрямую коррелирует в транскриптационной активностью данного участка ДНК. Типичный размер активного участка около 50 нуклеосом, таких участков около 10% от всего генома.
(-500A-50B-500A-50В-)
Блок-сополимерная модель хроматина
Мономерное звено
Структура последовательности
Блок A – слипающиеся звенья

## Slide 11
(500A50B)20
Genome Research, 26, 70 (2016)
Влияние природы взаимодействия
Стандартные объемные взаимодействия
Насыщающиеся взаимодействия

## Slide 12
Влияние структуры последовательности
Последовательность: 1000A-100B-(100A-10B)10-100B-1000A
Карта расстояний
конформация
Внедрение небольшой доли коротких блоков дополнительно стабилизирует домены, действуя как ПАВ.
Nucleus, 7 (3), 319 (2016)

## Slide 13
Взаимодействие с ламиной (клеточной мембраной)
Около 30% от всего хроматина
Находится неподалеку от
поверхности ядра
При этом домены намного более
плотные и плоские, что дает
дополнительный объем
активно работающим генам

## Slide 14
Микрогели: что это?
Microgels
Не вполне ясна их внутренняя структура и от чего она зависит.

## Slide 15
Моделирование химической реакции полимеризации
Всего в системе несколько типов частиц: мономеры, сшиватели, инициаторы.

## Slide 16
Процесс синтеза микрогелей в динамике
Начальная конфигурация: все равномерно растворено
100M steps
800M steps
Conversion
Зародыш
Готовая частицы
В реальном лабораторном эксперименте этот процесс идет от нескольких минут до нескольких дней

## Slide 17
Влияние констант реакции:
17
Структура микрогелей
Возможно прямое сопоставление с данными рассеяния

## Slide 18
Взаимопроникающие микрогели
Soft Matter, 2018, 14, 2777

## Slide 19
Самоорганизация в процессе полимеризации
А что будет не в бесконечно разбавленном растворе?

## Slide 20
Обнаружены новые фазы в области концентрированного раствора!
Самоорганизация в процессе полимеризации

## Slide 21
Микрофазное расслоение в блоксополимерах
Notes: Whu did I talk about PIL? Obviously, we can take block copolymers out of PIL, for example, diblock, one block is PIL, another not. Block copolymers are known for Another very popular topic to be studied using DPD is microphase separation in copolymers. In short, if you have a copolmer with chemically incompatible blocks because of the chain connectivity , in a melt it would not be able to form two big macrophases as a mixture of homopolymers would do but rather will split into microphases of different morphology depending on the chain architecture. The classical ones are … Microphase separated nanostructured systems have a number advantages compared to homogeneous ones: different phases can have different properties, for instance, one can make the material mechanically stable and tough, while the other can have good ion conductivity

## Slide 22
Визуализация микрофазного расслоения
Notes: Again the effect can be studied in dynamics: here you can see a video of how a lamellar strucutre is formed. You can see how the domains merge to form one gigantic one.

## Slide 23
Заряженные блоки стремятся отделиться от незаряженных, чтобы увеличить корреляции со своими противоионами
Влияние имеющихся зарядов
Невозможно достаточно корректно аналитически описать этот процесс.
Notes: Let’s get back to pils. If we consider a diblock-copolymer with one block made of pil, due to the aforementioned charge correlation attraction such blocks will attract. This seems like an additional froce which leads to the microphase separation

## Slide 24
Электростатические взаимодействия: неожиданные проблемы
Точечные заряды бесконечно сближаются из за отсутствия жесткого исключенного объема
Notes: While the introduction of electrostatic forces in molecular dynamics seems obvious, for DPD everything is bad. Since we do not have the hard-core potential such as LJ, the beads can overlap completely and the energetic penalty for that is finite. But the energetic gain from the coulomb interactions betwwen oppositely charged beads can be infinite, which will lead to charge collapsing onto each other.

## Slide 25
Как выбрать оптимальную функцию?

## Slide 26: Расчет дальнодействующих электростатических взаимодействий: PPPM
Long-range part is solved on a lattice

## Slide 27
Фазовая диаграмма
χ=0!
Расслоение возможно даже если исходно (без зарядов) все было гомогенно
Notes: . So the system is diblock copolymer with one charged block. The charge correlation effects cause the charged block with counterions to form a condensed phase. Sepending on the fraction of the charged block different structures can be observed, including

## Slide 28: Выводы
In silico методы дают гораздо более строгий ответ, чем аналитические приближения.
In silico методы гораздо проще интерпретировать, чем лабораторные эксперименты.
Уже сейчас есть много примеров, когда in silico методики дают новые знания и ведут за собой постановку новых лабораторных экспериментов и построение аналитического описания.

## Slide 29: Избранные публикации из top25%, с благодарностями суперкомпьютеру, отмечены авторы с логинами
[1] | D. V. Guseva, V. Y. Rudyak, P. V. Komarov, A. V. Sulimov, B. A. Bulgakov, and A. V. Chertovich, Journal of Polymer Science, Part B: Polymer Physics, vol. 58, no. 5, pp. 362–374, 2018.
[2] | D. V. Guseva, V. Y. Rudyak, P. V. Komarov, B. A. Bulgakov, A. V. Babkin, and A. V. Chertovich, Polymers, vol. 10, p. 792, 2018.
[3] | R. Shupanov, A. Chertovich, and P. Kos, Journal of Computational Chemistry, 2018.
[4] | V. Y. Rudyak, A. A. Gavrilov, E. Y. Kozhunova, and A. V. Chertovich, Soft Matter, vol. 14, pp. 2777–2781, 2018.
[5] | A. Kaznacheev, E.Pozhidaev, V.Rudyak, A. Emelyanenko, and A.Khokhlov, Physical Review E, vol. 97, no. 4, p. 042703, 2018.
[6] | A. A. Gavrilov and I. I. Potemkin, Soft Matter, vol. 14, no. 24, pp. 5098–5105, 2018.
[7] | Y. D. Gordievskaya, A. A. Gavrilov, and E. Y. Kramarenko, Soft Matter, vol. 14, pp. 1474–1481, 2018.
[8] | S. A. Shvetsov, V. Y. Rudyak, A. V. Emelyanenko, N. I. Boiko, Z. Yan-Song, L. Jui-Hsiang, and A. R. Khokhlov, Journal of Molecular Liquids, 2018.
[9] | M. N. Krakhalev, A. P. Gardymova, O. O. Prishchepa, V. Y. Rudyak, A. V. Emelyanenko, L. Jui-Hsiang, and V. Y. Zyryanov, Scientific reports, vol. 7, p. 14582, 2017.
[10] | V. Y. Rudyak, M. N. Krakhalev, V. S. Sutormin, O. O. Prishchepa, V. Y. Zyryanov, L. J-H, A. V. Emelyanenko, and A. R. Khokhlov, Physical Review E, vol. 96, pp. 052701–1–052701–5, 2017.
[11] | A. A. Gavrilov and A. V. Chertovich, Macromolecules, vol. 50, no. 12, pp. 4677–4685, 2017.
[12] | E. Y. Kozhunova, A. A. Gavrilov, M. Y. Zaremski, and A. V. Chertovich, Langmuir, vol. 33, no. 14, pp. 3548–3555, 2017.
[13] | A. V. Sergeev, A. V. Chertovich, D. M. Itkis, S. Anik, G. Axel, and A. R. Khokhlov, Journal of Physical Chemistry C, vol. 121, no. 27, pp. 14463–14469, 2017.
[14] | A. A. Gavrilov, A. V. Chertovich, and E. Y. Kramarenko, Macromolecules, vol. 49, no. 3, pp. 1103–1110, 2016.
[15] | D. V. Guseva, A. V. Chertovich, and V. Y. Rudyak, Journal of Chemical Physics, vol. 145, no. 14, p. 144503, 2016.
[16] | B. A. Bulgakov, A. V. Babkin, P. B. Dzhevakov, A. A. Bogolyubov, A. V. Sulimov, A. V. Kepman, Y. G. Kolyagin, D. V. Guseva, V. Y. Rudyak, and A. V. Chertovich, European Polymer Journal, no. 84, pp. 205–217, 2016.
[17] | A. V. Sergeev, A. V. Chertovich, and D. M. Itkis, Chemical Physics Letters, vol. 660, pp. 149–154, 2016.
[18] | A. A. Gavrilov, A. V. Chertovich, and E. Y. Kramarenko, Journal of Chemical Physics, vol. 145, no. 17, pp. 174101–1–174101–10, 2016.
Всего с 2016 года 25 статей с благодарностью суперкомпьютерному комплексу

## Slide 30
Коллектив:
Артем Сергеев, Павел Кос, Александр Чертович, Алексей Гаврилов, Владимир Рудяк
Лаборатория микроструктурированных полимерных материалов
mspslab.com
Физический факультет МГУ
кафедра физики полимеров и кристаллов.

## Slide 31: Dissipative particle dynamics method
bead
31
Notes: Let’s move to dissipative particle dymanics. It’s a coarse-grained version of molecular dynamics. This tech- nique is based on the simulation of soft spheres, whose mo- tion is governed by certain collision rules. all particles interact by three forces. It was shown that the dissipative force and the random force have to satisfy a certain relation in order that the system has the statistical mechanics corresponding to the canonical en- semble with a temperature related to the relative amplitudes of the random and dissipative interactions.
As compared to usual molecular dynamics simulations, for example with Lennard-Jones atoms, the major advantage of the DPD method is its soft interaction potential FC. Such a soft force can be considered as a mean effective force arising from averaging the interactions between the groups which compise each beads over time and orientations. Soft potential allows for a much larger timestep than is commonly used in usual MD simulations because the force does not diverge at any distance.

## Slide 32: Program technical details
2D Domain decomposition method was used to parallelize the program code.
2D decomposition technique is a balanced method for supercomputers with average
internal network quality
Notes: In the domain decomposition technique [1,5,6,7] each process calculates forces and integrates the coordinates of the particles within certain fixed region of space defined at the beginning of a simulation. If a particle leaves the region of space "belonging" to some process, all information is transferred to the corresponding process. This method of parallelization allows exchanges at the local level, resulting in a much better speed-up on a large number of processes (Fig. 1). However, the calculation of the bonds forces, which nature is non-local, leads to a deviation from the linear acceleration when using very large number of processes (>512).

## Slide 33
33
Electrostatic interactions in DPD: Problem solution
Groot, R. D. J. Chem. Phys. 2003, 118, 11265.
Usage of smeared charges is the solution
The potential no longer diverges at r=0
Re
Re
Notes: It was proposer by groot to use smeared charges instead of point-like ones. It seems very logical, as from hard-core volume intaractions we moved to soft-core interactions, so for the electrostatic interactions it’s desirable to do the same. The linear smearing funtion was proposed , so the amount of charge is proportional to r going to 0 at some value called smearing radius Re. The potential no longer diverges at r=0, but there are some energetic deviations at small distances.

## Slide 34
34
Applications: single polyelectrolyte chain
Gavrilov, A. A.; Chertovich, A. V.; Kramarenko, E. Y. Macromolecules 2016, 49, 1103–1110.
Different chain state is observed for different types of counterions
Notes: The properties of a single chain have also been studied in DPD. In our recent work we compared we studied the influence of conterion type on the chain collapse. The size of the small counterions was equal to the size of a monomer unit, while the bulky counterions were modeled as big spherical particles with twice the radius of a monomer unit. Two cases of the charge location within the bulky counterions were studied: (i) in the center (symmetrical case) or (ii) on the counterion surface (asymmetrical case). In agreement with the previous works, at low electrostatic strengths (λ<1) the polymer chain swells; upon increasing λ it starts to shrink, and eventually forms a dense globular state (λ≥2.5) due to the charge correlation effects At high charge fractions the chains with both small counterions and symmetrical bulky counterions collapsed at large electrostatic strengths . In contrast, the chain with asymmetrical bulky counterions did not collapse at all; instead, it adopted swollen conformations with counterions strongly attached to the chain backbone

## Slide 35
35
How to choose the smearing size?
One can study the screening properties in a bulk electrolyte at different salt concentrations in order to determine whether the screening length corresponds to the theoretical one
But… At high concentrations this approach is bad because the screening length becomes too small and deviations from the theoretical behavior can be observed
One can choose the electrostatic force so that the charge correlation effects are reproduced correctly. The charge correlation effects are important for the properties of a wide range of systems starting from simple liquid electrolytes to complex biological molecules
Notes: In a system with charges it is energetically more favorable for the charges positions on average to be correlated rather than to be completely random.
Some of these systems possess very inhomogeneous charge distributions; it is characteristic for polyelectrolyte systems where the average charge concentration might be low, but due to the charges being connected in a polymer chain a local charge concentration can be rather high. So it seems rather important to be able to simulate electrostatic interactions at even the smallest length scale.

## Slide 36
36
How to choose the smearing size?
Charge compensating
Notes: Let me show you what I mean. If the charge density is high enough, the charge clouds start to penetrate into each other. While for two charges the drawback is an obvious error in energy, for system like this the effect of charge compensating is completely unclear and may lead to incorrect physice

## Slide 37
37
Verification: single chain collapse
One can see a perfect quantitative agreement between the MD data and the DPD data at all studied λ
Notes: And it is possible! If one chooses the electroststic force correcty one can keep all the advantages of DPD and at the same time study the electostatic effects corersctly. This slide shows again the dependence of the chain size on the electrostatic strength, but this time in comparison with the molecular dynamics simulation data, where due to the hard-core nature of the volume interactions in MD, non-smoothed Coulomb potential was used. And we can see a perfect agreement between the MD and DPD data and also there is a green curve showing how the chain behaves if the commonly used paramateres for smoothing are used.

## Slide 38
Poly(ionic liquids)
Poly(ionic liquids) are a special type of polyelectrolytes which carry an IL species in each of the repeating units – the IL is basically attached to the polymer chain
38
Notes: In short, polyionic liquids are a special type of polyelectrolytes which carry an IL species in each of the repeating units[3]. Such architecture allows one to combine the advantages of polymers and ionic liquids in one material. For instance, the “classical” polymer electrolytes could not play the role of solid ion conductors: due to the extensive ion-pairing only materials with very low bulk conductivity are usually obtained in absence of a polar solvent. A good example of such behavior is a well-known material Nafion, which conducts only swollen in a significant amount of water. This problem is not present for poly (ionic liquids), as they demonstrate a very high ionic conductivity in the “dry” state (without solvent), which significantly improves the mechanical properties of such conducting materials.

## Slide 39
Shaplov, A. S.; Marcilla, R.; Mecerreyes, D. Electrochim. Acta 2015, 175, 18–34.
Poly(ionic liquids)
Such systems have been shown to have good conductivities and mechanical stability
39
Notes: Moreover, there are a lot of types of anions and cations which can be used, and the resulting polymer material can conduct either cations or anions depending on which ion is linked to the polymer. This picture shows only a small fraction of systems with cross-linked cations available now. All these circumstances allow one to finely tune the properties of the system.

## Slide 40
40
How to choose the smearing size?
?
Advantage of using large smearing radii:
Less computationally demanding as coarser mesh could be used
Disadvantage of using large smearing radii:
Unexpected simulation artifacts due to incorrect physics
Notes: But all those functions have a parameter discribing how wide the distribution is. That parameter is usially considered as a “technical”. Is this completely true? Which rises a question: how to choose the smearing size? What should one take in mind? Well, there is a very huge advantage of using large smearing radii. But, as it always happens, there is a disadvantage as well

## Slide 41
Microphase separation in polymer melts
41
Gavrilov, A. A.; Kudryavtsev, Y. V.; Chertovich, A. V. J. Chem. Phys. 2013, 139 (22), 224901.
Matsen // Macromolecules 45 (2012) 2161